## Slide 1
Manufacturers of Cutting edge SMT Stencils, Carrier Pallets, Wave Solder Pallets and High Precision Laser Cut components.

## Slide 2: Introduction
• We are Apertronics Private Limited.
• Located near Bangalore, India
We introduce ourselves as next generation SMT Stencil and Tooling manufacturers.

## Slide 3: Our Vision
•“To be a world-class manufacturer of next generation high precision laser- cut products and SMT tooling.”

## Slide 4: Mission Statement
•We will strive for continuous improvement in our technical capabilities in providing high quality products that meet and exceed our customer’s requirements and ensure complete satisfaction.

## Slide 5: Current Industry Trends
•PCB’s are getting denser and more complex, IC’s are getting smaller with every generation, BGA’s are becoming common.
•The requirements of SMT Stencil are becoming more and more demanding day by day

## Slide 6: Type of SMT Stencils
• Basic stencil with multiple frame sizes.
• Step up/down & Multi-step stencils
(No theoretical limit on number of Steps)
• Nickel stencils
• Micro-Shield(nano coating) stencil
• Nano slic gold stencil
• Frameless stencil(Tetra-Bond)
• Mini stencil for rework.

## Slide 7
Basic Stencil- with Multiple Frame Sizes
● 29” by 29”
● 23” by 23”
● 650 mm by 550 mm
● 680mm by 650 mm
● 22” by 22”
● 20” by 20”
● 1350 mm by 500mm
● Customised sizes

## Slide 8: Step up/down & Multi-Step stencils
Maximum Step Difference upto 10 Mils and no changes in surface texture

## Slide 9: Next Gen technology for step up/down stencils
Step down
Step up

## Slide 10: Next Gen technology for step up/down stencils
Manufacturing time 3-4 hours maximum
Step tolerance 2-3 microns
Squeegee damage significantly reduced
No change in the texture of the Stainless Steel
Solder paste release is excellent

## Slide 11: Aperture cutting in side wall
No bur in side the wall

## Slide 12: Nickel stencil
Our Nickel Stencils offer:
• High accuracy and repeatability
• Enhanced ultra fine pitch capability(5 Mil Gap)
• Reduced under-stencil cleaning requirements, due
to positive underside gasketing
• Transfer efficiency is optimised in cases of critical Surface Area(SA) ratio
• Stepped area(s) have optimized paste volume
deposit
• Long stencil life – up to twice that of stainless steel stencils
• Nickel stencils can also be shipped the same day, depending on approval and stock availability

## Slide 13: Micro Shield(Nano Coated) Stencil

## Slide 14: Nano slic gold Stencil
World's Most Advanced Stencil Coating NanoSlic offers the world's most advanced coating for solder paste stencils. The NanoSlic Stencil Coating System is a turn-key system that integrates surface preparation, coating and curing to provide unparalleled printing improvements, transfer efficiency and ease-of-cleaning.

## Slide 15: Aperture wall

## Slide 16: After 25000 print

## Slide 17: After 50000 print

## Slide 18: After 75000 prints

## Slide 19: After 100000 prints

## Slide 20: Nano slic coating in aperture wall

## Slide 21: Frameless stencil- TetraBond
Advantages:
● Space saving(⅓ rd space needed)
● Latest generation design
● Moulded Pre-Hard Anodised frame

## Slide 22: Mini stencils for Rework

## Slide 23: Stencil inspection report(AOI)
Detects clogged apertures or debris that can impact printing integrity, as well as checking aperture dimension, presence, position and area. Area ratio is also calculated.

## Slide 24: Carrier Pallets
Benefits:
• Reduces setup time
• Eliminates unnecessary PCB handling by operators
• Minimizes PCB warpage
• Eliminates expensive hand masking and related labor costs
• Standardizes process repetition
• Machine parameters can be fixed
• Minimizes soldering defects

## Slide 25: Wave Solder Pallets
Benefits:
• Reduces setup time
• Used to solder complex, double-sided
PCBA’s
• Eliminates expensive and labor-intensive masking
• Shields heat-sensitive components
• Processes multiple boards at the same time
• Reduces bridging and skipping
• Increases rate of production and supports automated assembly operations.

## Slide 26: Thank you
Contact us:
Email: sales@apertronics.com Phone: + 91 6384027001
www.apertronics.com